Comments on ARB staff report: Proposed Airborne Toxic Control Measure to Reduce Formaldehyde Emissions from Composite Wood Products.

Reference to Appendix H:

I think the preferred Japanese test method is the JIS A 1901 ( chamber method) not the desicator method JIS A 1460. See page 18 in the Japanese Amended Standard Building Law (2003) document. This document can be retrieved at http://www.jetro.go.jp/en/jetro/facilities/housing/legal_system/top/index.html

The JIS 1901 can also be more directly compared with the ASTM E1333 and EN 717-1. The JIS A 1460 specifies relatively low test temperature 20C and high humidity 65%. This low temperature is below the emission threshold for many materials containing formaldehyde resins. Also the desicator is a static measurement (no air exchange). This is why the Japanese Government is moving to the JIS A 1901.

Below is an updated chart which compares the different methods on an emission rate basis and ppm basis. I have not tried to account for differences in the way edges of samples are treated.  The only way this can accurately be done is to run side by side tests with the same test system.  I have use the JIS A 1901 for the Japanese F*** standard.

Comparisons of Formaldehyde Emission Rates Required for Various International Certification Standards

Regal Air Quality, Inc.

Updated March 14,2007

| Test Program | ARB 2009 | ARB 2011 | ARB 2009 | ARB 2011 | ARB 2009 | ARB 2011 | E-1 | Japan F*** |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Building Product | PB | PB | HWPW | HWPW | MDF | MDF | PB,MDF,HWPW | PB |
| Test Method | ASTM-E1333 | ASTM-E1333 | ASTM-E1333 | ASTM-E1333 | ASTM-E1333 | ASTM-E1333 | EN-717-1 | JIS A 1901 |
| Test Temperature | 25C | 25C | 25C | 25C | 25C | 25C | 23 C | 28C |
| Test RH | 50% | 50% | 50% | 50% | 50% | 50% | 45% | 50% |
| Chamber Volume, m3 | 28 | 28 | 28 | 28 | 28 | 28 | 0.22 | 1 |
| Air Change Rate, h-1 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 0.5 | 1.0 | 0.5 |
| Loading Factor LA, m2/m3 | 0.425 | 0.425 | 0.95 | 0.95 | 0.26 | 0.26 | 1.0 | 2.2 |
| Acceptable HCHO Concentration, µg m-3 | <220 | < 110 | <46 | <28 | <333 | <174 | < 120 | N.A. |
| SERA , µg m-2h-1 | <259 | <110 | <46 | <28 | <333 | <174 | <120 | < 20 |
| *SER Corrected to 25C | <259 | <110 | <46 | <28 | <333 | <174 | <150 | < 14.4 |
| ASTM E-1333 ppm | 0.18 | 0.09 | 0.08 | 0.05 | 0.21 | 0.11 | 0.12 | 0.05 |

* Formaldehyde Emission Corrected for Temperature Using Equation in ASTM D 6007-02

References:

Building Center of Japan. 2004. Performance Testing  and Evaluation Manual for Emission Rate of Formaldehyde from Building Materials., Building Center of Japan, BR-BO-11-02

Building Guidance Div. Japanese Government. 2003, Building Standard Law Restriction on VOC Emission etc. Retrievable at

http://www.jetro.go.jp/en/jetro/facilities/housing/legal_system/top/index.html

Risholm, M, A .Larsen, E.Vestin, and A.Weibull. 2006 Formaldehyde Emission- A comparison of different standard methods. Accepted for publication in the Journal of Atmospheric Environment.

Risholm, Maria.2006-2007 Personal Communication. Use of Japanese standard JSA 1901       .